## Slide 1
Potential of Low Gain Avalanche Detectors (LGAD) for Plasma Diagnostics in pB Fusion Experiments
5th International Workshop on Proton-Boron Fusion
September 8-11, 2025, Belgrade, Serbia
Milos Manojlovic, Neil Moffat, Gordana Lastovicka-Medin, Martin Perez, Pablo Fernández-Martínez, Enric Cabruja, Salvador Hidalgo, Giulio Pellegrini
Contact e-mail: milos.manojlovic@imb-cnm.csic.es

## Slide 2: Outline
Motivation
  History & Why detectors with multiplication?
State of the art
  Low Gain Avalanche Diodes (LGAD)
  Ultra-fast silicon detectors (UFSD)
    4D tracking
Gain response (chosen examples)
  MIPs, protons, neutrons, X-rays, ions, photons …
Future
  LGADs in pB fusion experiments?

## Slide 3: How it all started? …
Silicon detectors
Severe radiation
Charge
MULTIPLICATION
Question was (<2010):
Can we then build Si-based detectors with multiplication mechanism & could they be used as fast timing detectors?

## Slide 4: ATLAS, LHC & HL-LHC (CERN) context …
√s = 13.6 TeV
About 1.1 × 10¹¹ protons per bunch
40 million bunch crossings per second
Up to 10¹⁶ particles per cm² over HL-LHC lifetime hitting the innermost detectors
Signal
Pile-up!
PROBLEM…

## Slide 5: Ultra-fast silicon detectors for 4D tracking (x, y, z, t)
Track particles in space coordinates
  Good spatial resolution (10 um for example)
  Track particles in time (10s of picosecond)
Low Gain Avalanche Detectors technology …
  Thin
p++
p-
n++
E-profile
+
p+
p++
p-
n++
E-profile
+
PiN diode
LGAD
SOLUTION…
We also use Boron ;)

## Slide 6: Low Gain Avalanche Detector
[1] A.G. Stewart et al. in Proc. of SPIE, Vol. 6119, 2006
No Gain
Moderate Gain
&
Proportional response
Gain > 104
Digital response
Linear mode
  Proposed by IMB-CNM in 2014
  Proportional response (linear mode operation)
  Better sensitivity (Gain)
  S/N ratio increased
  Excellent timing resolution (~ 30 ps)
  MIP detection for HEP
  Thin detector integration with the same signal and higher collection efficiency
Original paper
G. Pellegrini, et al., Technology developments and first measurements of Low Gain Avalanche Detectors (LGAD) for high energy physics applications, Nucl. Instrum. Methods A 765 (2014) 12.

## Slide 7: State-of-the-art…
Low Gain Avalanche Diodes (LGAD)

## Slide 8
When a reverse bias is applied:
Detector depletes (Free of charge carriers)
Electric field present which attracts electrons to the N++ contact (TOP)
Holes move to P++
High field region at junction between P++ and N+ region
P-type LGAD

## Slide 9
Charge particle interaction in device
(By photons, electrons, protons, X-rays….)
P-type LGAD
From fusion, why not?

## Slide 10
Electron-hole pair generated due to interaction
P-type LGAD

## Slide 11
Electrons move up
Holes move down
P-type LGAD

## Slide 12
Electrons move up
Holes move down
P-type LGAD

## Slide 13
When electron reaches high field (Gain Region) it is accelerated and undergoes impact ionisation
P-type LGAD

## Slide 14
Electrons are collected (almost) instantaneously
Holes drift to bottom side
P-type LGAD

## Slide 15
Electrons are collected (almost) instantaneously
Holes drift to bottom side
P-type LGAD

## Slide 16
Electrons are collected (almost) instantaneously
Holes drift to bottom side
P-type LGAD

## Slide 17
Electrons are collected (almost) instantaneously
Holes drift to bottom side
P-type LGAD

## Slide 18: P-type LGAD
Electrons are collected (almost) instantaneously
Holes drift to bottom side

## Slide 19: In LGAD …
Many LGAD ”flavours” are emerging depending on the application

## Slide 20: LGAD vs nLGAD
Pellegrini et al, European patent EP 3 971 997 B1
Villegas et al, TREDI 2024
Villegas et al, https://doi.org/10.1016/j.nima.2025.170208
Pellegrini et al, https://doi.org/10.1016/j.nima.2014.06.008
Electron-driven multiplication
Gain of LGAD is penetration depth-dependant

## Slide 21: Some results on nLGAD (photon detection)
[1] Villegas, J., Torres, C., Manojlovic, M., Jimenez-Ramos, M. C., Moffat, N., Lopez, J. G., & Hidalgo, S. (2025). NLGAD gain response to low-penetrating particles. Nuclear Instruments and Methods in Physics Research Section A: Accelerators, Spectrometers, Detectors and Associated Equipment, 1072, 170208. https://doi.org/10.1016/j.nima.2025.170208
[2] Manojlović, M., Moffat, N., Fernandez-Martínez, P., Villegas, J., Cabruja, E., Rebarz, M., Pellegrini, G., & Hidalgo, S. (2025). nLGAD detector gain response to deep and near-ultraviolet (UV) light. [Manuscript submitted for publication]
Deep-UV light
(250 nm)
Wavelength [nm]
Submitted…
250
404
Gain
15
5
21
X
│
R
A
Y
280 < E < 530 eV
Water window range
H2O
T ~ 1
A ~ 1
A – Absorptance coefficient T – Transmittance coefficient
- Carbon
- Oxygen
Medical Imaging Application
SOFT X-RAY
Ultra-shallow junction nLGAD (USJ-nLGAD)

## Slide 22: Examples (LGADs & nLGAD)… what we know…
Angular measurements (600 keV protons)
α-particle in fusion experiments
n
10B+n→7Li+α+Q
Q = 2.79 MeV
α
Proton detection
Ion detection
Could have implications in pB fusion experiment
Gain
Gain
Gain
Gain
Voltage [V]
Can LGADs be used for neutron detection in pB fusion?
What we want to test…
Alpha particle detection (source)

## Slide 23
Andreo Crnjac et. al.

## Slide 24: pB fusion context…
[1] Margarone, D. et al. (2022) ‘In-target proton–boron nuclear fusion using a PW-class laser’, Applied Sciences, 12(3), p. 1444. doi:10.3390/app12031444.
1p +11B →34He +8.7MeV
Aneutronic (almost no neutrons)
Direct energy conversion (charged particles)
maximum of 1011 α/sr/shot[2]
[2] McKenzie, Warren, et al. “HB11—Understanding Hydrogen-Boron Fusion as a New Clean Energy Source.” Journal of Fusion Energy, vol. 42, no. 1, 13 May 2023, https://doi.org/10.1007/s10894-023-00349-9. Accessed 24 Aug. 2023.
LGAD is radiation resistant with this neutron flux
[1] Sen Zhao, Keqi Wang, Kaibo Xie, Chenxi Fu, Chengwei Wang, Xin Shi and Congcong Wang, Charge Collection Performance of 4H-SiC LGAD, IEEE TRANSACTIONS ON NUCLEAR SCIENCE, VOL. XX, NO. XX, XXXX 2020
The community working on
4H-SiC LGAD

## Slide 25: Nothing is perfect…
LGADs suffer from gain loss under severe radiation environments
  Acceptor removal mechanism (ARM) (well studied)
  Donor removal mechanism (we are investigating it…) [1]
[1] Milos Manojlovic, Andreo Crnjac, Neil Moffat, et al. Gain Response and Ion Beam-Induced Donor Removal in nLGAD Detector: Global Gain Quenching. TechRxiv. September 04, 2025. DOI: 10.36227/techrxiv.175699542.28031525/v1
N(ф) = N(0) exp(−CA ф)
10¹⁵ neq/cm² (1 MeV neutron equivalent fluence)
Mitigation teckniques: Carbon co-implantation, compensation design etc.
Margarita Biveinytė, Marcos Fernandez Garcia, Salvador Hidalgo, Veronika Kraus, Michael Moll, Jairo Villegas, Moritz Wiehe, Characterization and Irradiation Studies of the Novel nLGAD Concept, VCI2025

## Slide 26: Experiment in October
"PROton BOron Nuclear fusion: from energy production to medical applications" (PROBONO - CA21128) (Dr. Przemysław Tchórz)
LGAD detector systems for neutrons and charged particles: isntallation, opetration, and data analysis (Dr. Gordana Lastovicka-Medin)
Feasibility study…

## Slide 27
Applications
Collaboration & Ideas 
Femtosecond-scale dynamics Attosecond laser experiments?
Soft X-ray imaging
UV-light detection
in space research
Deep-UV detection
In nuclear fusión experiments
Gamma radiation detection
HL-LHC phase CERN
In October at ELI The feasibiluty study

## Slide 28: Acknowledgements
Acknowledgements
This work has been funded by the Spanish Ministry of Science and Innovation (MCIN/AEI/10.13039/501100011033/) and by the European Union’s ERDF program “A way of making Europe”. Grant references: PID2020-113705RB-C32 and PID2021-124660OB-C22. Also, it was funded by the European Union’s Horizon 2020 Research and Innovation funding program, under Grant Agreement No. 101004761 (AIDAInnova).
Thank you!